Bobrick offers seven types of toilet partitions and over 750 products for public washroom facilities.  Please view the Full Catalog at www.bobrick.com or contact your local representative for assistance, by calling 818-503-1600 or by searching on our website by state or country.

This specification section is provided in CSI-format, and intended to be included in the Project Manual for a construction project.  Delete models and options not required for your project, and modify to your project requirements.  © 1970-2014 Bobrick Washroom Equipment, Inc.

SECTION 102113

TOILET COMPARTMENTS

GENERAL

SECTION INCLUDES

Solid Color Reinforced Composite (SCRC) Substrate:  (Bobrick SierraSeries®)

Toilet Partitions:

Configuration:  Floor-Anchored, Overhead-Braced.

Configuration:  Floor-to-Ceiling.

Configuration:  Ceiling-Hung.

Urinal Privacy Screens:

Configuration:  Post-to-Ceiling.

Configuration:  Wall-Hung.

Dressing Compartments:  Floor-Anchored, Overhead-Braced.

Shower Dividers:  Floor-Anchored, Overhead-Braced.

Compact Laminate, Moisture Resistant Substrate:  (Bobrick DuraLineSeries®)

Toilet Partitions:

Configuration:  Floor-Anchored.

Configuration:  Floor-Anchored, Overhead-Braced.

Configuration:  Floor-to-Ceiling.

Configuration:  Ceiling-Hung.

Urinal Privacy Screens:

Configuration:  Floor-Anchored.

Configuration:  Post-to-Ceiling.

Configuration:  Wall-Hung.

Configuration:  Ceiling-Hung.

Dressing Compartments:  Floor-Anchored, Overhead-Braced.

Shower Dividers:  Floor-Anchored, Overhead-Braced.

High Pressure Laminate Substrate:  (Bobrick ClassicSeries®)

Toilet Partitions:

Configuration:  Floor-Anchored.

Configuration:  Floor-Anchored, Overhead-Braced.

Configuration:  Ceiling-Hung.

Urinal Privacy Screens:

Configuration:  Floor-Anchored.

Configuration:  Wall-Hung.

Configuration:  Ceiling-Hung.

Dressing Compartments:  Floor-Anchored, Overhead-Braced.

High Pressure Laminate Substrate:  (Bobrick MetroSeries™)

Toilet Partitions:

Configuration:  Floor-Anchored.

Configuration:  Floor-Anchored, Overhead-Braced.

Configuration:  Ceiling-Hung.

Urinal Privacy Screens:

Configuration:  Floor-Anchored.

Configuration:  Wall-Hung.

Configuration:  Ceiling-Hung.

Dressing Compartments:  Floor-Anchored, Overhead-Braced.

High Pressure Laminate Substrate:  (Bobrick AccentSeries™)

Toilet Partitions:

Configuration:  Floor-Anchored.

Configuration:  Floor-Anchored, Overhead-Braced.

Configuration:  Ceiling-Hung.

Urinal Privacy Screens:

Configuration:  Floor-Anchored.

Configuration:  Wall-Hung.

Configuration:  Ceiling-Hung.

Dressing Compartments:  Floor-Anchored, Overhead-Braced.

High Pressure Laminate Substrate with Steel Core Reinforced Stiles:  (Bobrick DesignerSeries™)

Toilet Partitions:

Configuration:  Floor-Anchored.

Configuration:  Floor-Anchored, Overhead-Braced.

Configuration:  Ceiling-Hung.

Urinal Privacy Screens:

Configuration:  Floor-Anchored.

Configuration:  Post-to-Ceiling.

Configuration:  Wall-Hung.

Configuration:  Ceiling-Hung.

Dressing Compartments:  Floor-Anchored, Overhead-Braced.

High Pressure Laminate Substrate with Steel Core Reinforced Stiles And Stainless Steel Edge Trim:  (Bobrick TrimLineSeries™)

Toilet Partitions:

Configuration:  Floor-Anchored.

Configuration:  Floor-Anchored, Overhead-Braced.

Configuration:  Ceiling-Hung.

Urinal Privacy Screens:

Configuration:  Floor-Anchored.

Configuration:  Post-to-Ceiling.

Configuration:  Wall-Hung.

Configuration:  Ceiling-Hung.

Dressing Compartments:  Floor-Anchored, Overhead-Braced.

RELATED REQUIREMENTS

Section 055000 - Metal Fabrications, coordination with overhead supports; steel beams above finished ceiling to secure Ceiling-Hung and floor-to-ceiling stiles.

Section 061000 - Rough Carpentry, coordination with blocking in walls to secure panels, wall posts and stiles.

Section 095000 - Ceilings, coordination with layout and installation.

Section 092000 - Plaster and Gypsum Board, coordination with blocking.

Section 093000 - Tiling, coordination with layout and installation.

Section 102800 - Washroom Accessories, for accessories.

Section 102814 - Baby Changing Stations, for baby changing stations.

SUBMITTALS

Product Data:  Submit manufacturer's data sheets for each product specified.

Shop Drawings:  Submit manufacturer’s shop drawings for each product specified, including the following:

Plans, elevations, details of construction and attachment to adjacent construction.

Show anchorage locations and accessory items.

Verify dimensions with field measurements prior to final production of toilet compartments.

USGBC LEED Submittals:

For Bobrick ClassicSeries, MetroSeries, AccentSeries, DesignerSeries, TrimlineSeries and DuraLineSeries:  Materials and Resource Credits MR4.1 and MR4.2 - Recycled Content; submit manufacturer’s calculation of value of recycled content for specified products, calculated in accordance with USGBC LEED certification requirements.

For Bobrick ClassicSeries, MetroSeries, AccentSeries, DesignerSeries, TrimlineSeries, DuraLineSeries, and SierraSeries:  Materials and Resource Credits MR5.1 and MR5.2 – Regional Materials; submit manufacturer’s calculation of value of recycled content for specified products, calculated in accordance with USGBC LEED certification requirements.

For Bobrick ClassicSeries, MetroSeries, AccentSeries, DesignerSeries and TrimLineSeries:  Materials and Resource Credit MR6 - Rapidly Renewable Materials; submit manufacturers certification that products contain raw materials that are derived from plants that are harvested within a 10 year cycle or shorter.

For Bobrick ClassicSeries, MetroSeries, AccentSeries, DesignerSeries, TrimLineSeries, DuralineSeries:  Materials and Resource Credit MR7- Certified Wood; submit manufacturers certification that a minimum of 50% of wood based materials are certified in accordance with Forest Stewardship Council (FSC) Guidelines.

For Bobrick SierraSeries:  Indoor Environmental Quality Credit IEQ 4 - No Added Urea Formaldehyde; submit manufacturer’s certification that composite and agrifiber products contain no added urea-formaldehyde resins and that laminating used to fabricate on-site and shop-applied composite wood and agrifiber contain no added urea-formaldehyde resins.

For Bobrick SierraSeries:  Indoor Environmental Quality Credit IEQ 4 for Schools; submit manufacturer’s certification that products comply with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

USA Certificate of Origin: Manufacturer must supply with first submittal, an example of their Certificate of Origin declaring toilet compartments are wholly manufactured and assembled specifically in the United States, including city and state locations. A notarized Certificate of Origin must be provided with closeout documents.

QUALITY ASSURANCE

Manufacturer:  Provide products manufactured by a company with a minimum of 10 years successful experience manufacturing similar products.

Single Source Requirements:  To the greatest extent possible provide products from a single manufacturer.

Accessibility Requirements:  Comply with requirements applicable in the jurisdiction of the project, including but not limited to ADA and ICC/ANSI A117.1 requirements as applicable.

DELIVERY, STORAGE, AND HANDLING

Deliver, store and handle materials and products in strict compliance with manufacturer's instructions and recommendations.  Protect from damage.

WARRANTY

Manufacturer’s Warranty (SierraSeries):  Manufacturer’s standard 25 year limited warranty for panels, doors, and stiles against breakage, corrosion, and defects in factory workmanship.  Manufacturer’s standard 1 year guarantee against defects in material and workmanship for stainless steel door hardware and mounting brackets.

Manufacturer’s Warranty (DuraLineSeries):  Manufacturer’s standard 25 year limited warranty for panels, doors, and stiles against breakage, corrosion, delamination, and defects in factory workmanship.  Manufacturer’s standard 1 year guarantee against defects in material and workmanship for stainless steel door hardware and mounting brackets.

Manufacturer’s Warranty (ClassicSeries):  Manufacturer’s standard 2 year warranty for materials and workmanship.  Manufacturer’s standard 1 year guarantee against defects in material and workmanship for door hardware and mounting brackets.

Manufacturer’s Warranty (MetroSeries):  Manufacturer’s standard 2 year warranty for materials and workmanship.  Manufacturer’s standard 1 year guarantee against defects in material and workmanship for door hardware and mounting brackets.

Manufacturer’s Warranty (AccentSeries):  Manufacturer’s standard 5 year warranty for materials and workmanship. Manufacturer’s standard 1 year guarantee against defects in material and workmanship for stainless steel door hardware and mounting brackets

Manufacturer’s Warranty (DesignerSeries):  Manufacturer’s standard 2 year warranty for materials and workmanship. Manufacturer’s standard 1 year guarantee against defects in material and workmanship for stainless steel door hardware and mounting brackets

Manufacturer’s Warranty (TrimLineSeries):  Manufacturer’s standard 5 year warranty for materials and workmanship.  Manufacturer’s standard 1 year guarantee against defects in material and workmanship for stainless steel door hardware and mounting brackets

PRODUCTS

MANUFACTURER

Basis-of-Design Products: Based on the quality and performance requirements of the project, specifications are based solely on the products of Bobrick Washroom Equipment, Inc..  www.bobrick.com.  Location of manufacturing shall be the United States.

Substitutions:  The Architect will consider products of comparable manufacturers as a substitution, pending the contractor's submission of adequate documentation of the substitution in accordance with procedures in Division 1 of the Project Manual.  Documentation shall include a list of five similar projects of equivalent size where products have been installed for a minimum of two years, and manufacturer's certification that products are fabricated in the United States.

SOLID COLOR REINFORCED COMPOSITE (SCRC) SUBSTRATE (SierraSeries)

Solid Color Reinforced Composite (SCRC) Partitions:  Bobrick SierraSeries.

Color:  As selected by Architect from manufacturer’s standard SierraSeries range.

Color:  As indicated on Drawings.

Color:  SC01 Golden Khaki.

Color:  SC02 Desert Beige.

Color:  SC03 Terra Cotta.

Color:  SC04 Forest Green.

Toilet Partitions:

Configuration:  Overhead-Braced partitions; with satin finish, extruded anodized aluminum headrails, 0.065 inch (1.65 mm) thick with anti-grip profile.

Basis-of-Design:  Bobrick 1092 SierraSeries Toilet Partitions.

Design:  Standard design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 1092G SierraSeries Toilet Partitions, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 1092.67 SierraSeries Toilet Partitions, vandal resistant.

Design:  Standard design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Basis-of-Design:  Bobrick 1092G.67 SierraSeries Toilet Partitions, vandal resistant, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Basis-of-Design:  Bobrick 2092 SierraSeries Toilet Partitions, maximum height.

Design:  Standard design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 2092G SierraSeries Toilet Partitions, maximum height, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 2092.67 SierraSeries Toilet Partitions, maximum height, vandal resistant.

Design:  Standard design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Basis-of-Design:  Bobrick 2092G.67 SierraSeries Toilet Partitions, maximum height, vandal resistant, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Configuration:  Floor-to-ceiling partitions.

Basis-of-Design:  Bobrick 1096 SierraSeries Toilet Partitions.

Design:  Standard design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 1096G SierraSeries Toilet Partitions, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 1096.67 SierraSeries Toilet Partitions, vandal resistant.

Design:  Standard design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Basis-of-Design:  Bobrick 1096G.67 SierraSeries Toilet Partitions, vandal resistant, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Basis-of-Design:  Bobrick 2096 SierraSeries Toilet Partitions, maximum height.

Design:  Standard design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 2096G SierraSeries Toilet Partitions, maximum height, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 2096.67 SierraSeries Toilet Partitions, maximum height, vandal resistant.

Design:  Standard design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Basis-of-Design:  Bobrick 2096G.67 SierraSeries Toilet Partitions, maximum height, vandal resistant, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Configuration:  Ceiling-Hung partitions, 10 ft (3048 mm) maximum ceiling height.

Basis-of-Design:  Bobrick 1098 SierraSeries Toilet Partitions.

Design:  Standard design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 1098G SierraSeries Toilet Partitions, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 1098.67 SierraSeries Toilet Partitions, vandal resistant.

Design:  Standard design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Basis-of-Design:  Bobrick 1098G.67 SierraSeries Toilet Partitions, vandal resistant, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Basis-of-Design:  Bobrick 2098 SierraSeries Toilet Partitions, maximum height.

Design:  Standard design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 2098G SierraSeries Toilet Partitions, maximum height, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 2098.67 SierraSeries Toilet Partitions, maximum height vandal resistant.

Design:  Standard design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Basis-of-Design:  Bobrick 2098G.67 SierraSeries Toilet Partitions, maximum height, vandal resistant, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Fire Resistance:

Flame Spread Index (ASTM E 84):  45 for panels, doors and stiles.

Smoke Developed Index (ASTM E 84):  120 for panels, 95 for doors and stiles.

National Fire Protection Association/International Building Code Interior Wall and Ceiling Finish:  Class B.

Uniform Building Code:  Class II.

Urinal Privacy Screens:

Basis-of-Design:  Bobrick 1093 SierraSeries Post-to-Ceiling Urinal Privacy Screens.

Posts:  18-8, Type 304, 18 gauge (1.2 mm) stainless steel with satin finish; 1.25 inch (32 mm) square, 10 ft (3048 mm) lengths field cut to required height.

Basis-of-Design:  Bobrick 1095 SierraSeries Wall-Hung Urinal Privacy Screens.

Brackets:  11 gauge (3 mm), double thickness.

Hardware:  To match partition hardware.

Fire Resistance:

Flame Spread Index (ASTM E 84):  45 for panels and stiles.

Smoke Developed Index (ASTM E 84):  120 for panels, 95 for stiles.

National Fire Protection Association/International Building Code Interior Wall and Ceiling Finish:  Class B.

Uniform Building Code:  Class II.

Dressing Compartments:  Floor-Anchored, Overhead-Braced.

Basis-of-Design:  Bobrick 1092 SierraSeries Dressing Compartments.

Design:  Standard design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 2092 SierraSeries Dressing Compartments, maximum height.

Design:  Standard design.

Hardware:  Standard hardware.

Headrails:  Standard headrails, extruded anodized aluminum with satin finish, 0.065 inch (1.65 mm) thick with anti-grip profile.

Headrails:  Headrail with integral curtain tracks and hooks for compartments without doors.

Curtains:  Optional Bobrick vinyl curtains.

Fire Resistance:

Flame Spread Index (ASTM E 84):  45 for panels and stiles.

Smoke Developed Index (ASTM E 84):  120 for panels, 95 for stiles.

National Fire Protection Association/International Building Code Interior Wall and Ceiling Finish:  Class B.

Uniform Building Code:  Class II.

Shower Dividers:  Floor-Anchored, Overhead-Braced.

Basis-of-Design:  Bobrick 1092 SierraSeries Shower Dividers.

Design:  Standard design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 2092 SierraSeries Shower Dividers, maximum height.

Design:  Standard design.

Hardware:  Standard hardware.

Headrails:  Standard headrails, extruded anodized aluminum with satin finish, 0.065 inch (1.65 mm) thick with anti-grip profile.

Headrails:  Headrail with integral curtain tracks and hooks for compartments without doors.

Curtains:  Optional Bobrick vinyl curtains.

Fire Resistance:

Flame Spread Index (ASTM E 84):  45 for panels and stiles.

Smoke Developed Index (ASTM E 84):  120 for panels, 95 for stiles.

National Fire Protection Association/International Building Code Interior Wall and Ceiling Finish:  Class B.

Uniform Building Code:  Class II.

Materials:  Solid color reinforced composite (SCRC) material for stiles, panels, doors, and screens with Bobrick GraffitiOff® coating, thermoset and integrally fused into homogenous piece; high density polyethylene (HDPE), high density polypropylene not acceptable.

Composition:  Dyes, organic fibrous material, and polycarbonate/phenolic resins.

Surface Treatment:  Non-ghosting, graffiti resistant surface integrally bonded to core through a series of manufacturing steps requiring thermal and mechanical pressure.

Edges:  Same color as the surface.

Acceptable SCRC Products:  Or manufacturer approved equal.

Ultimate Corian System by Shower Shapes.

WilsonArt Gibraltar Material.

WilsonArt EarthStone Material.

Performance Requirements:

Graffiti Resistance (ASTM D 6578): Passed cleanability test; 5 staining agents.

Scratch Resistance (ASTM D 2197):  Maximum load value exceeds 10 kilograms.

Impact Resistance (ASTM D 2794): Maximum impact force exceeds 30 inch-pounds.

Smoke Developed Index (ASTM E 84):  Less than 450.

Flame Spread Index (ASTM E 84):  Less than 75.

Finished Thickness:

Stiles and Doors:  3/4 inch (19 mm)

Finished thickness of doors and stiles to ensure flush front.

Panels and Screens:  1/2 inch (13 mm).

Stiles: Floor-Anchored stiles furnished with expansion shields and threaded rods.

Leveling Devices:  7 gauge, 3/16 inches (5 mm) thick, corrosion-resistant, chromate-treated, double zinc-plated steel angle leveling bar bolted to stile; furnished with 3/8 inch (10 mm) diameter threaded rods, hex nuts, lock washers, flat washers, spacer sleeves, expansion anchors, and shoe retainers.

Stile Shoes:  One-piece, 22 gauge (0.8 mm), 18-8, Type 304 stainless steel, 4 inch (102 mm) height; tops with 90 degree return to stile.  One-piece shoe capable of adapting to 3/4 inch (19 mm) or 1 inch (25 mm) stile thickness and capable of being fastened (by clip) to stiles starting at wall line.

Wall Posts:  Pre-drilled for door hardware, 18-8, Type 304, 16 gauge (1.6 mm) stainless steel with satin finish; 1 inch (25 mm) x 1-1/2 inches (38 mm) x 58 inches high (1473 mm).

Anchors:  Expansion shields and threaded rods at floor connections as applicable.  Threaded rods secured to supports above ceiling as applicable.  Supports above ceiling furnished and installed as Work of Section 055000.

Hardware:

Compliance:  Operable with one hand, without tight grasping, pinching, or twisting of the wrist, and force to operate does not exceed five pounds.

Emergency Access:  Hinges, latch allow door to be lifted over keeper from outside compartment on inswing doors.

Materials:  18-8, Type 304, heavy-gauge stainless steel with satin finish. Chrome-plated “Zamak”, aluminum, or extruded plastic hardware not acceptable.

Fastening:  Hardware secured to door and stile by through-bolted, theft-resistant, pin-in-head Torx stainless steel machine screws into factory-installed, threaded brass inserts.  Fasteners secured directly into core not acceptable.

Threaded Brass Inserts:  Factory-installed; withstand direct pull force exceeding 1500 lb (680 kg) per insert.

Clothes Hooks:  Projecting no more than 1-1/8 inch (29 mm) from face of door.

Hardware Type:  Standard, commercial hardware.

Latching:  Track of door latch prevents inswing doors from swinging out beyond stile; on outswing doors, door keeper prevents door from swinging in beyond stile; 14 gauge (2 mm) sliding door latch, 11 gauge (3.2 mm) keeper.  Twist-style door latch operation not acceptable.

Hinges:  Balanced, with field-adjustable cam to permit door to be fully closed or partially open when compartment is unoccupied.

Locking:  Door locked from inside by sliding door latch into keeper.

Mounting Brackets:  Mounted inside compartment; exposed brackets on exterior of compartment not acceptable with the exception of outswing doors.

Hardware Type:  Institutional Hardware (.67).

Latching:  14 gauge (2 mm) sliding door latch, 11 gauge (3.2 mm) keeper; latch slides on a shock-resistant nylon track.  Twist-style door latch operation not acceptable.

Hinges:  16 gauge (1.6 mm) stainless steel, self-closing, 3 section hinges.

Mounting Brackets:  18 gauge (1.2 mm) stainless steel and extend full height of panel.

U-Channels:  Secure panels to stiles.

Angle Brackets:  Secure stiles-to-walls and panels-to-walls.

COMPACT LAMINATE, MOISTURE RESISTANT SUBSTRATE (DuraLineSeries)

Compact Laminate, Moisture Resistant Partitions:  Bobrick DuraLineSeries.

Color:  As selected by Architect from manufacturer’s standard DuraLineSeries range.

Color:  As indicated on Drawings.

Color:  515-58 Graphite Grafix.

Color:  851-58 Spectrum Blue.

Color:  909-58 Black.

Color:  949-58 White.

Color:  3518-58 Flint Crystal.

Color:	 4674 Evening Tigris.

Color:  4872-60 Western Storm.

Color:  4878-60 Pewter Mesh.

Color:  7022-58 Natural Canvas.

Color:  P-500 BlackStar.

Color:  P-886 Grey Grit.

Color:  P-887 Beige Grit.

Color:  S-431 Willow Grey.

Color:  S-436 Sand.

Color:  S-445 Almond.

Color:  S-463 Antique White.

Color:  S-513 Denim Blue.

Color:  S-542 Limousine Grey.

Toilet Partitions:

Configuration:  Floor-Anchored partitions.

Basis-of-Design:  Bobrick 1181 DuraLineSeries Toilet Partitions.

Design:  Standard design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 1181G DuraLineSeries Toilet Partitions, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 1181.67 DuraLineSeries Toilet Partitions, vandal resistant.

Design:  Standard design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Basis-of-Design:  Bobrick 1181G.67 DuraLineSeries Toilet Partitions, vandal resistant, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Basis-of-Design:  Bobrick 2181 DuraLineSeries Toilet Partitions, maximum height.

Design:  Standard design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 2181G DuraLineSeries Toilet Partitions, maximum height, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 2181.67 DuraLineSeries Toilet Partitions, maximum height, vandal resistant.

Design:  Standard design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Basis-of-Design:  Bobrick 2181G.67 DuraLineSeries Toilet Partitions, maximum height, vandal resistant, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Configuration:  Floor-Anchored, Overhead-Braced partitions; satin finish; extruded anodized aluminum headrails with satin finish, 0.065 inch (1.65 mm) thick with anti-grip profile.

Basis-of-Design:  Bobrick 1182 DuraLineSeries Toilet Partitions.

Design:  Standard design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 1182G DuraLineSeries Toilet Partitions, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 1182.67 DuraLineSeries Toilet Partitions, vandal resistant.

Design:  Standard design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Basis-of-Design:  Bobrick 1182G.67 DuraLineSeries Toilet Partitions, vandal resistant, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Basis-of-Design:  Bobrick 2182 DuraLineSeries Toilet Partitions, maximum height.

Design:  Standard design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 2182G DuraLineSeries Toilet Partitions, maximum height, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 2182.67 DuraLineSeries Toilet Partitions, maximum height, vandal resistant.

Design:  Standard design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Basis-of-Design:  Bobrick 2182G.67 DuraLineSeries Toilet Partitions, maximum height, vandal resistant, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Configuration:  Floor-to-ceiling partitions.

Basis-of-Design:  Bobrick 1186 DuraLineSeries Toilet Partitions.

Design:  Standard design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 1186G DuraLineSeries Toilet Partitions, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 1186.67 DuraLineSeries Toilet Partitions, vandal resistant.

Design:  Standard design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Basis-of-Design:  Bobrick 1186G.67 DuraLineSeries Toilet Partitions, vandal resistant, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Basis-of-Design:  Bobrick 2186 DuraLineSeries Toilet Partitions, maximum height.

Design:  Standard design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 2186G DuraLineSeries Toilet Partitions, maximum height, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 2186.67 DuraLineSeries Toilet Partitions, maximum height, vandal resistant.

Design:  Standard design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Basis-of-Design:  Bobrick 2186G.67 DuraLineSeries Toilet Partitions, maximum height, vandal resistant, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Configuration:  Ceiling-Hung partitions, 10 ft (3048 mm) maximum ceiling height.

Basis-of-Design:  Bobrick 1188 DuraLineSeries Toilet Partitions.

Design:  Standard design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 1188G DuraLineSeries Toilet Partitions, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 1188.67 DuraLineSeries Toilet Partitions, vandal resistant.

Design:  Standard design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Basis-of-Design:  Bobrick 1188G.67 DuraLineSeries Toilet Partitions, vandal resistant, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Basis-of-Design:  Bobrick 2188 DuraLineSeries Toilet Partitions, maximum height.

Design:  Standard design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 2188G DuraLineSeries Toilet Partitions, maximum height, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 2188.67 DuraLineSeries Toilet Partitions, maximum height, vandal resistant.

Design:  Standard design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Basis-of-Design:  Bobrick 2188G.67 DuraLineSeries Toilet Partitions, maximum height, vandal resistant, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Fire Resistance:

Flame Spread Index (ASTM E 84):  15 for panels, doors and stiles.

Smoke Developed Index (ASTM E 84):  25 for panels, 20 for doors and stiles.

National Fire Protection Association/International Building Code Interior Wall and Ceiling Finish:  Class A.

Uniform Building Code:  Class I.

Toilet Partitions:

Configuration:  Floor-Anchored partitions.

Basis-of-Design:  Bobrick 1081 DuraLineSeries Toilet Partitions.

Design:  Standard design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 1081G DuraLineSeries Toilet Partitions, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 1081.67 DuraLineSeries Toilet Partitions, vandal resistant.

Design:  Standard design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Basis-of-Design:  Bobrick 1081G.67 DuraLineSeries Toilet Partitions, vandal resistant, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Basis-of-Design:  Bobrick 2081 DuraLineSeries Toilet Partitions, maximum height.

Design:  Standard design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 2081G DuraLineSeries Toilet Partitions, maximum height, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 2081.67 DuraLineSeries Toilet Partitions, maximum height, vandal resistant.

Design:  Standard design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Basis-of-Design:  Bobrick 2081G.67 DuraLineSeries Toilet Partitions, maximum height, vandal resistant, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Configuration:  Floor-Anchored, Overhead-Braced partitions;.

Basis-of-Design:  Bobrick 1082 DuraLineSeries Toilet Partitions.

Design:  Standard design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 1082G DuraLineSeries Toilet Partitions, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 1082.67 DuraLineSeries Toilet Partitions, vandal resistant.

Design:  Standard design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Basis-of-Design:  Bobrick 1082G.67 DuraLineSeries Toilet Partitions, vandal resistant, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Basis-of-Design:  Bobrick 2082 DuraLineSeries Toilet Partitions, maximum height.

Design:  Standard design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 2082G DuraLineSeries Toilet Partitions, maximum height, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 2082.67 DuraLineSeries Toilet Partitions, maximum height, vandal resistant.

Design:  Standard design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Basis-of-Design:  Bobrick 2082G.67 DuraLineSeries Toilet Partitions, maximum height, vandal resistant, gap-free; extruded anodized aluminum headrails with satin finish, 0.065 inch (1.65 mm) thick with anti-grip profile.

Design:  Gap-free interlocking design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Configuration:  Floor-to-ceiling partitions.

Basis-of-Design:  Bobrick 1086 DuraLineSeries Toilet Partitions.

Design:  Standard design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 1086G DuraLineSeries Toilet Partitions, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 1086.67 DuraLineSeries Toilet Partitions, vandal resistant.

Design:  Standard design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Basis-of-Design:  Bobrick 1086G.67 DuraLineSeries Toilet Partitions, vandal resistant, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Basis-of-Design:  Bobrick 2086 DuraLineSeries Toilet Partitions, maximum height.

Design:  Standard design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 2086G DuraLineSeries Toilet Partitions, maximum height, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 2086.67 DuraLineSeries Toilet Partitions, maximum height, vandal resistant.

Design:  Standard design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Basis-of-Design:  Bobrick 2086G.67 DuraLineSeries Toilet Partitions, maximum height, vandal resistant, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Configuration:  Ceiling-Hung partitions, 10 ft (3048 mm) maximum ceiling height.

Basis-of-Design:  Bobrick 1088 DuraLineSeries Toilet Partitions, maximum height.

Design:  Standard design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 1088G DuraLineSeries Toilet Partitions, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 1088.67 DuraLineSeries Toilet Partitions, vandal resistant.

Design:  Standard design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Basis-of-Design:  Bobrick 1088G.67 DuraLineSeries Toilet Partitions, vandal resistant, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Basis-of-Design:  Bobrick 2088 DuraLineSeries Toilet Partitions, maximum height.

Design:  Standard design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 2088G DuraLineSeries Toilet Partitions, maximum height, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 2088.67 DuraLineSeries Toilet Partitions, maximum height, vandal resistant.

Design:  Standard design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Basis-of-Design:  Bobrick 2088G.67 DuraLineSeries Toilet Partitions, maximum height, vandal resistant, gap-free.

Design:  Gap-free interlocking design.

Hardware:  Vandal resistant full-height stainless steel hardware.

Fire Resistance:

Flame Spread Index (ASTM E 84):  30 for panels, doors and stiles.

Smoke Developed Index (ASTM E 84):  55 for panels, 20 for doors and stiles.

National Fire Protection Association/International Building Code Interior Wall and Ceiling Finish:  Class B.

Uniform Building Code:  Class II.

Urinal Privacy Screens:

Basis-of-Design:  Bobrick 1181 DuraLineSeries Floor-Anchored Urinal Privacy Screens.

Basis-of-Design:  Bobrick 1183 DuraLineSeries Post-to-Ceiling Urinal Privacy Screens.

Posts:  18-8, Type 304, 18 gauge (1.2 mm) stainless steel with satin finish; 1.25 inch (32 mm) square, 10 ft (3048 mm) lengths field cut to required height.

Basis-of-Design:  Bobrick 1185 DuraLineSeries Wall-Hung Urinal Privacy Screens.

Basis-of-Design:  Bobrick 1188 DuraLineSeries Ceiling-Hung Urinal Privacy Screens.

Hardware:  To match partition hardware.

Fire Resistance:

Flame Spread Index (ASTM E 84):  15 for panels and stiles.

Smoke Developed Index (ASTM E 84):  25 for panels, 20 for stiles.

National Fire Protection Association/International Building Code Interior Wall and Ceiling Finish:  Class A.

Uniform Building Code:  Class I.

Urinal Privacy Screens:

Basis-of-Design:  Bobrick 1081 DuraLineSeries Floor-Anchored Urinal Privacy Screens.

Basis-of-Design:  Bobrick 1083 DuraLineSeries Post-To-Ceiling Urinal Privacy Screens.

Posts:  18-8, Type 304, 18 gauge (1.2 mm) stainless steel with satin finish; 1.25 inch (32 mm) square, 10 ft (3048 mm) lengths field cut to required height.

Basis-of-Design:  Bobrick 1085 DuraLineSeries Wall-Hung Urinal Privacy Screens.

Brackets:  11 gauge (3 mm), double thickness.

Basis-of-Design:  Bobrick 1088 DuraLineSeries Ceiling-Hung Urinal Privacy Screens.

Hardware:  To match partition hardware.

Fire Resistance:

Flame Spread Index (ASTM E 84):  30 for panels and stiles.

Smoke Developed Index (ASTM E 84):  55 for panels, 20 for stiles.

National Fire Protection Association/International Building Code Interior Wall and Ceiling Finish:  Class B.

Uniform Building Code:  Class II.

Dressing Compartments:  Floor-Anchored, Overhead-Braced.

Basis-of-Design:  Bobrick 1182 DuraLineSeries Dressing Compartments.

Design:  Standard design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 2182 DuraLineSeries Dressing Compartments, maximum height.

Design:  Standard design.

Hardware:  Standard hardware.

Headrails:  Standard headrails; extruded anodized aluminum with satin finish, 0.065 inch (1.65 mm) thick with anti-grip profile.

Headrails:  With integral curtain tracks and hooks for compartments without doors.

Provide optional Bobrick vinyl curtains.

Fire Resistance:

Flame Spread Index (ASTM E 84):  15 for panels and stiles.

Smoke Developed Index (ASTM E 84):  25 for panels, 20 for stiles.

National Fire Protection Association/International Building Code Interior Wall and Ceiling Finish:  Class A.

Uniform Building Code:  Class I.

Dressing Compartments:  Floor-Anchored, Overhead-Braced.

Basis-of-Design:  Bobrick 1082 DuraLineSeries Dressing Compartments.

Design:  Standard design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 2082 DuraLineSeries Dressing Compartments, maximum height.

Design:  Standard design.

Hardware:  Standard hardware.

Headrails:  Standard headrails; extruded anodized aluminum with satin finish, 0.065 inch (1.65 mm) thick with anti-grip profile.

Headrails:  With integral curtain tracks and hooks for compartments without doors.

Provide optional Bobrick vinyl curtains.

Fire Resistance:

Flame Spread Index (ASTM E 84):  30 for panels and stiles.

Smoke Developed Index (ASTM E 84):  55 for panels, 20 for stiles.

National Fire Protection Association/International Building Code Interior Wall and Ceiling Finish:  Class B.

Uniform Building Code:  Class II.

Shower Dividers:  Floor-Anchored, Overhead-Braced.

Basis-of-Design:  Bobrick 1182 DuraLineSeries Shower Dividers.

Design:  Standard design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 2182 DuraLineSeries Shower Dividers, maximum height.

Design:  Standard design.

Hardware:  Standard hardware.

Headrails:  Standard headrails; extruded anodized aluminum with satin finish, 0.065 inch (1.65 mm) thick with anti-grip profile.

Headrails:  With integral curtain tracks and hooks for compartments without doors.

Provide optional Bobrick vinyl curtains.

Fire Resistance:

Flame Spread Index (ASTM E 84):  15 for panels and stiles.

Smoke Developed Index (ASTM E 84):  25 for panels, 20 for stiles.

National Fire Protection Association/International Building Code Interior Wall and Ceiling Finish:  Class A.

Uniform Building Code:  Class I.

Shower Dividers:  Floor-Anchored, Overhead-Braced.

Basis-of-Design:  Bobrick 1082 DuraLineSeries Shower Dividers.

Design:  Standard design.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 2082 DuraLineSeries Shower Dividers, maximum height.

Design:  Standard design.

Hardware:  Standard hardware.

Headrails:  Standard headrails; extruded anodized aluminum with satin finish, 0.065 inch (1.65 mm) thick with anti-grip profile.

Headrails:  With integral curtain tracks and hooks for compartments without doors.

Provide optional Bobrick vinyl curtains.

Fire Resistance:

Flame Spread Index (ASTM E 84):  30 for panels and stiles.

Smoke Developed Index (ASTM E 84):  55 for panels, 20 for stiles.

National Fire Protection Association/International Building Code Interior Wall and Ceiling Finish:  Class B.

Uniform Building Code:  Class II.

Materials:  Compact Laminate material for stiles, panels, doors and screens.

Phenolic Construction:  Solidly fused high pressure laminate with matte-finish melamine surfaces; integrally bonded colored face sheets and black phenolic-resin core.

Phenolic Edges:  Black; brown edges not acceptable.

Finished Thickness:

Stiles and Doors:  3/4 inch (19 mm).

Finished thickness of doors and stiles to ensure flush front.

Panels and Screens:  1/2 inch (13 mm).

Wall Posts:  Pre-drilled for door hardware, 18-8, Type 304, 16 gauge (1.6 mm) stainless steel with satin finish; 1 inch (25 mm) x 1-1/2 inches (38 mm) x 58 inches high (1473 mm).

Stiles:  Floor-Anchored stiles furnished with expansion shields and threaded rods.

Leveling Devices:  7 gauge, 3/16 inches (5 mm) thick, corrosion-resistant, chromate-treated, double zinc-plated steel angle leveling bar bolted to stile; furnished with 3/8 inch (10 mm) diameter threaded rods, hex nuts, lock washers, flat washers, spacer sleeves, expansion anchors, and shoe retainers.

Stile Shoes:  One-piece, 22 gauge (0.8 mm), 18-8, Type 304 stainless steel, 4 inch (102 mm) height; tops with 90 degree return to stile.  One-piece shoe capable of adapting to 3/4 inch (19 mm) or 1 inch (25 mm) stile thickness and capable of being fastened (by clip) to stiles starting at wall line.

Anchors:  Expansion shields and threaded rods at floor connections as applicable.  Threaded rods secured to supports above ceiling as applicable.  Supports above ceiling furnished and installed as Work of Section 055000.

Hardware:

Compliance:  Operable with one hand, without tight grasping, pinching, or twisting of the wrist, and force to operate does not exceed five pounds.

Emergency Access:  Hinges, latch allow door to be lifted over keeper from outside compartment.

Materials:  18-8, Type 304, heavy-gauge stainless steel with satin finish.  Chrome-plated “Zamak”, aluminum, or extruded plastic hardware not acceptable.

Fastening:  Hardware secured to door and stile by through-bolted, theft-resistant, pin-in-head Torx stainless steel machine screws into factory-installed, threaded brass inserts.  Fasteners secured directly into core not acceptable.

Threaded Brass Inserts:  Factory-installed; withstand direct pull force exceeding 1500 lb (680 kg) per insert.

Clothes Hooks:  Projecting no more than 1-1/8 inch (29 mm) from face of door.

Mounting: Hinges, keepers, latches, clothes hooks and their fasteners concealed inside compartment.  Exposed hinges, keepers, latches, clothes hooks and their fasteners on exterior of compartment not acceptable with the exception of accessible compartments.

Hardware Type:  Standard, commercial hardware.

Latching: Track of door latch prevents inswing doors from swinging out beyond stile; on outswing doors, door keeper prevents door from swinging in beyond stile; 14 gauge (2 mm) sliding door latch, 11 gauge (3.2 mm) keeper. Black rubber bumper on latch serves as door bumper for inswing door.  Twist-style door latch operation not acceptable.

Hinges:  Balanced, with field-adjustable cam to permit door to be fully closed or partially open when compartment is unoccupied.

Locking:  Door locked from inside by sliding door latch into keeper.

Mounting Brackets:  Mounted inside compartment; exposed brackets on exterior of compartment not acceptable with the exception of outswing doors.

Hardware Type:  Institutional hardware (.67).

Latching:  14 gauge (2 mm) sliding door latch, 11 gauge (3.2 mm) keeper; latch slides on shock-resistant nylon track. Twist-style door latch operation not acceptable.

Hinges:  16 gauge (1.6 mm) stainless steel with satin finish, self-closing, 3 section hinges.

Mounting Brackets:  18 gauge (1.2 mm) stainless steel and extend full height of panel.

U-Channels:  Secure panels to stiles.

Angle Brackets:  Secure stiles-to-walls and panels-to-walls.

HIGH PRESSURE LAMINATE SUBSTRATE  (ClassicSeries)

High Pressure Laminate Partitions:  Bobrick ClassicSeries.

Color:  As selected by Architect from manufacturer’s standard ClassicSeries range.

Color:  As indicated on Drawings.

Color:  As selected by Architect from manufacturer’s 2 Day Lead Time ClassicSeries range.

Color:  As selected by Architect from manufacturer’s 5 Day FastColor ClassicSeries range.

Color:  1500-60 Grey

Color:  1530-60 Beige

Color:  1572-60 Antique White

Color:  1595-60 Black

Color:  3690-58 Basalt Slate

Color:  4177-58 Lime

Color:  4622-60 Grey Nebula

Color:  4623-60 Graphite Nebula

Color:  4667-60 Green Tigris

Color:  4669-60 Natural Tigris

Color:  4674-60 Evening Tigris

Color:  4794-60 Windswept Bronze

Color:  4814-60 Tungsten Ev

Color:  4830K-18 Satin Stainless

Color:  4841-60 Desert Zephyr

Color:  4848-38 Pewter Mesh

Color:  4859-60 Spiced Zephyr

Color:  4924-38 White Carrara

Color:  5881-58 Chocolate Warp

Color:  5884-58 Chestnut Woodline

Color:  6212-58 Wheat Strand

Color:  6214-58 Seagrass Strand

Color:  6307-58 Burnt Strand

Color:  7018-58 Navy Grafix

Color:  7022-58 Natural Canvas

Color:  7040A-60 Figured Mahogany

Color:  7945K-38 Xanadu

Color:  851-58 Spectrum Blue

Color:  D30-60 Natural Almond

Color:  D307-60 Hollyberry

Color:  D315-60 Platinum

Color:  D321-60 Brittany Blue

Color:  D354-60 Designer White

Color:  D91-60 Slate Grey

Color:  D96-60 Shadow

Toilet Partitions:

Configuration:  Floor-Anchored partitions.

Basis-of-Design:  Bobrick 1541 ClassicSeries Toilet Partitions.

Hardware:  Standard hardware.

Reinforcement:  None.

Basis-of-Design:  Bobrick 1541.63 ClassicSeries Toilet Partitions.

Hardware:  Standard hardware.

Reinforcement:  Steel core stiles, 11-gauge (3.2mm) sheet steel reinforcement; leveling device welded to sheet-steel core of stiles.

Configuration:  Floor-Anchored, Overhead-Braced partitions; extruded anodized aluminum with satin finish headrails, 0.045 inch (1.14 mm) thick with anti-grip profile.

Basis-of-Design:  Bobrick 1542 ClassicSeries Toilet Partitions.

Hardware:  Standard hardware.

Reinforcement:  None.

Basis-of-Design:  Bobrick 1542.63 ClassicSeries Toilet Partitions.

Hardware:  Standard hardware.

Reinforcement:  Steel core stiles, 11-gauge (3.2mm) sheet steel reinforcement; leveling device welded to sheet-steel core of stiles.

Configuration:  Ceiling-Hung partitions, 10 ft (3048 mm) maximum ceiling height.

Basis-of-Design:  Bobrick 1548 ClassicSeries Toilet Partitions.

Hardware:  Standard hardware.

Reinforcement:  None

Fire Resistance:

Flame Spread Index (ASTM E 84):  60 for panels, doors and stiles.

Smoke Developed Index (ASTM E 84):  300 for panels, doors and stiles.

National Fire Protection Association/International Building Code Interior Wall and Ceiling Finish:  Class B.

Uniform Building Code:  Class II.

Urinal Privacy Screens:

Basis-of-Design:  Bobrick 1541 ClassicSeries Floor-Anchored Urinal Privacy Screens.

Basis-of-Design:  Bobrick 1541.63 ClassicSeries Floor-Anchored Urinal Privacy Screens.

Reinforcement:  Steel core stiles, 11-gauge (3.2mm) sheet steel reinforcement; leveling device welded to sheet-steel core of stiles.

Basis-of-Design:  Bobrick 1545 ClassicSeries Wall-Hung Urinal Privacy Screens.

Basis-of-Design:  Bobrick 1548 ClassicSeries Ceiling-Hung Urinal Privacy Screens.

Hardware:  To match partition hardware.

Fire Resistance:

Flame Spread Index (ASTM E 84):  60 for panels and stiles.

Smoke Developed Index (ASTM E 84):  300 for panels and stiles.

National Fire Protection Association/International Building Code Interior Wall and Ceiling Finish:  Class B.

Uniform Building Code:  Class II.

Dressing Compartments:  Floor-Anchored, Overhead-Braced.

Basis-of-Design:  Bobrick 1542 ClassicSeries Dressing Compartments.

Hardware:  Standard hardware.

Reinforcement:  None.

Basis-of-Design:  Bobrick 1542.63 ClassicSeries Dressing Compartments.

Hardware:  Standard hardware.

Reinforcement:  Steel core stiles, 11-gauge (3.2mm) sheet steel reinforcement; leveling device welded to sheet-steel core of stiles.

Headrails:  Extruded anodized aluminum with satin finish, 0.045 inch (1.14 mm) thick with anti-grip profile.

Headrails:  Headrail with integral curtain tracks and hooks for compartments without doors.

Curtains:  Optional Bobrick vinyl curtains.

Fire Resistance:

Flame Spread Index (ASTM E 84):  60 for panels and stiles.

Smoke Developed Index (ASTM E 84):  300 for panels and stiles.

National Fire Protection Association/International Building Code Interior Wall and Ceiling Finish:  Class B.

Uniform Building Code:  Class II.

Finished Thickness:  1 inch (25 mm) for stiles, doors, screens and panels.  Finished thickness of doors and stiles to ensure flush front.

Materials:  3-ply, stiles, panels, doors, and screens.

Cores: 45 lb (20.4 kg) density, industrial grade, resin-impregnated, particle board.

Surfaces:  High Pressure Laminate ANSI/NEMA LD3-2005 minimum thickness 0.035 inch (0.89 mm).

Fabrication: High Pressure Laminate bonded to core material with adhesive specially formulated to prevent delamination.  Edges bonded prior to bonding face sheets.  Splices or joints in faces or edges are not acceptable except in the case of laminate material limitations.

Wall Posts:  Pre-drilled for door hardware, 18-8, Type 304, 16 gauge (1.6 mm) stainless steel with satin finish; 1 inch (25 mm) x 1-1/2 inches (38 mm) x 58 inches high (1473 mm).

Stiles:  Floor-Anchored stiles furnished with expansion shields and threaded rods.

Overhead Braced Leveling Devices:  12 gauge, 3 inch x 1.25 inch (75 mm x 32 mm) zinc plated steel with chromate treatment; factory installed to bottom of stile.

Floor-Anchored / Ceiling-Hung Leveling Devices:  12 gauge, 1/2 inch x 1 inch (13 mm x 25 mm) steel channel welded to 3/8 inch x 1 inch (10 mm x 25 mm) zinc-chromate plated steel bar.

Stile Shoes:  One-piece, 22 gauge (0.8 mm), 18-8, Type 304 stainless steel, 4 inch (102 mm) height; tops with 90 degree return to stile.  One-piece shoe capable of adapting to 3/4 inch (19 mm) or 1 inch (25 mm) stile thickness and capable of being fastened (by clip) to stiles starting at wall line.

Anchors:  Expansion shields and threaded rods at floor connections as applicable.  Threaded rods secured to supports above ceiling as applicable.  Supports above ceiling furnished and installed as Work of Section 055000.

Hardware:  Through-bolted hardware.

Compliance:  Operable with one hand, without tight grasping, pinching, or twisting of the wrist, and force to operate does not exceed five pounds.

Emergency Access:  Hinges, latch allow door to be lifted over keeper from outside compartment.

Latching:  Door is locked from inside by sliding door latch into keeper.  Twist-style door latch operation not acceptable.

Latch keeper:  Prevents inswing doors from swinging out beyond stile; on outswing doors, doorstop prevents door from swinging in beyond stile.

Hinges:  Pivot hinges; attached to door and stile by through-bolting theft-resistant, chrome one-way shoulder screws into one-way chrome barrel nuts.

Materials:  Chrome-plated “Zamak” for latches, hinges, coat hooks and bumpers, mounting brackets.

Combination coat hook and bumper reduces damage from door.

HIGH PRESSURE LAMINATE SUBSTRATE  (MetroSeries)

High Pressure Laminate Partitions:  Bobrick MetroSeries.

.

Color:  As selected by Architect from manufacturer’s standard MetroSeries range.

Color:  As indicated on Drawings.

Color:  As selected by Architect from manufacturer’s 2 Day Lead Time MetroSeries range.

Color:  As selected by Architect from manufacturer’s 5 Day FastColor MetroSeries range.

Color:  1500-60 Grey

Color:  1530-60 Beige

Color:  1572-60 Antique White

Color:  1595-60 Black

Color:  3690-58 Basalt Slate

Color:  4177-58 Lime

Color:  4622-60 Grey Nebula

Color:  4623-60 Graphite Nebula

Color:  4667-60 Green Tigris

Color:  4669-60 Natural Tigris

Color:  4674-60 Evening Tigris

Color:  4794-60 Windswept Bronze

Color:  4814-60 Tungsten Ev

Color:  4830K-18 Satin Stainless

Color:  4841-60 Desert Zephyr

Color:  4848-38 Pewter Mesh

Color:  4859-60 Spiced Zephyr

Color:  4924-38 White Carrara

Color:  5881-58 Chocolate Warp

Color:  5884-58 Chestnut Woodline

Color:  6212-58 Wheat Strand

Color:  6214-58 Seagrass Strand

Color:  6307-58 Burnt Strand

Color:  7018-58 Navy Grafix

Color:  7022-58 Natural Canvas

Color:  7040A-60 Figured Mahogany

Color:  7945K-38 Xanadu

Color:  851-58 Spectrum Blue

Color:  D30-60 Natural Almond

Color:  D307-60 Hollyberry

Color:  D315-60 Platinum

Color:  D321-60 Brittany Blue

Color:  D354-60 Designer White

Color:  D91-60 Slate Grey

Color:  D96-60 Shadow

Toilet Partitions:

Configuration:  Floor-Anchored partitions.

Basis-of-Design:  Bobrick 1551 MetroSeries Toilet Partitions.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 1551.64 MetroSeries Toilet Partitions.

Hardware:  Stainless steel hardware.

Configuration:  Floor-Anchored, Overhead-Braced partitions; extruded anodized aluminum with satin finish headrails, 0.045 inch (1.14 mm) thick with anti-grip profile.

Basis-of-Design:  Bobrick 1552 MetroSeries Toilet Partitions.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 1552.64 MetroSeries Toilet Partitions.

Hardware:  Stainless steel hardware

Configuration:  Ceiling-Hung partitions, 10 ft (3048 mm) maximum ceiling height.

Basis-of-Design:  Bobrick 1558 Metro Toilet Partitions.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 1558.64 MetroSeries Toilet Partitions.

Hardware:  Stainless steel hardware.

Fire Resistance:

Flame Spread Index (ASTM E 84):  60 for panels, doors and stiles.

Smoke Developed Index (ASTM E 84):  300 for panels, doors and stiles.

National Fire Protection Association/International Building Code Interior Wall and Ceiling Finish:  Class B.

Uniform Building Code:  Class II.

Urinal Privacy Screens:

Basis-of-Design:  Bobrick 1551 MetroSeries Floor-Anchored Urinal Privacy Screens.

Basis-of-Design:  Bobrick 1555 MetroSeries Wall-Hung Urinal Privacy Screens.

Basis-of-Design:  Bobrick 1558 MetroSeries Ceiling-Hung Urinal Privacy Screens.

Hardware:  To match partition hardware.

Fire Resistance:

Flame Spread Index (ASTM E 84):  60 for panels and stiles.

Smoke Developed Index (ASTM E 84):  300 for panels and stiles.

National Fire Protection Association/International Building Code Interior Wall and Ceiling Finish:  Class B.

Uniform Building Code:  Class II.

Dressing Compartments:  Floor-Anchored, Overhead-Braced.

Basis-of-Design:  Bobrick 1552 MetroSeries Dressing Compartments.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 1552.64 MetroSeries Dressing Compartments.

Hardware:  Stainless steel hardware.

Headrails:  Extruded anodized aluminum with satin finish, 0.045 inch (1.14 mm) thick with anti-grip profile.

Headrails:  Headrail with integral curtain tracks and hooks for compartments without doors.

Curtains:  Optional Bobrick vinyl curtains.

Fire Resistance:

Flame Spread Index (ASTM E 84):  60 for panels and stiles.

Smoke Developed Index (ASTM E 84):  300 for panels and stiles.

National Fire Protection Association/International Building Code Interior Wall and Ceiling Finish:  Class B.

Uniform Building Code:  Class II.

Finished Thickness:  1 inch (25 mm) for stiles, doors, screens and panels. Finished thickness of doors and stiles to ensure flush front.

Materials:  3-ply, stiles, panels, doors, and screens.

Cores: 45 lb (20.4 kg) density, industrial grade, resin-impregnated, particle board.

Surfaces:  High Pressure Laminate ANSI/NEMA LD3-2005 minimum thickness 0.035 inch (0.89 mm).

Fabrication:  High Pressure Laminate bonded to core material with adhesive specially formulated to prevent delamination.  Edges bonded prior to bonding face sheets.  Splices or joints in faces or edges are not acceptable except in the case of laminate material limitations.

Wall Posts:  Pre-drilled for door hardware, 18-8, Type 304, 16 gauge (1.6 mm) stainless steel with satin finish; 1 inch (25 mm) x 1-1/2 inches (38 mm) x 58 inches high (1473 mm).

Stiles:  Floor-Anchored stiles furnished with expansion shields and threaded rods.

Overhead Braced Leveling Devices:  12 gauge, 3 inch x 1.25 inch (75 mm x 32 mm) zinc plated steel with chromate treatment; factory installed to bottom of stile.

Floor-Anchored / Ceiling-Hung Leveling Devices:  12 gauge, 1/2 inch x 1 inch (13 mm x 25 mm) steel channel welded to 3/8 inch x 1 inch (10 mm x 25 mm) zinc-chromate plated steel bar.

Stile Shoes:  One-piece, 22 gauge (0.8 mm), 18-8, Type 304 stainless steel, 4 inch (102 mm) height; tops with 90 degree return to stile.  One-piece shoe capable of adapting to 3/4 inch (19 mm) or 1 inch (25 mm) stile thickness and capable of being fastened (by clip) to stiles starting at wall line.

Anchors:  Expansion shields and threaded rods at floor connections as applicable.  Threaded rods secured to supports above ceiling as applicable.  Supports above ceiling furnished and installed as Work of Section 055000.

Hardware:  Concealed hardware.

Compliance:  Operable with one hand, without tight grasping, pinching, or twisting of the wrist, and force to operate does not exceed five pounds.

Emergency Access:  Hinges, latch allow door to be lifted over keeper from outside compartment.

Fastening:  Hinges secured to door and stile by stainless steel screws fastened into factory-installed, threaded inserts.  Fasteners secured directly into core not acceptable.

Mounting: Hinges, keepers, latches, clothes hooks and their fasteners concealed inside compartment.  Exposed hinges, keepers, latches, clothes hooks and their fasteners on exterior of compartment not acceptable with the exception of accessible compartments.

Hinges:  Balanced, with field-adjustable cam to permit door to be fully closed or partially open when compartment is unoccupied

Mounting Brackets:  Mounted inside compartment; exposed brackets on exterior of compartment not acceptable with the exception of outswing doors.

Latching:  Door is locked from inside by sliding door latch into keeper.  Twist-style door latch operation not acceptable.

Standard Hardware

Materials:  Stainless steel with polished finish for hinges. Chrome-plated “Zamak” for latches, hinges, coat hooks and bumpers, mounting brackets.

Doorstop:  Prevents inswing doors from swinging out beyond stile; on outswing doors, keeper prevents door from swinging in beyond stile.

Combination coat hook and bumper provided to reduce damage from door.

Optional Hardware:  Stainless steel hardware (.64).

Materials:  Stainless steel with satin finish for latches, hinges, coat hooks and bumpers, mounting brackets.

b. 	Doorstop:  Integrated into inswing latch to prevent doors from swinging out beyond stile; On outswing and alcove doors, doorstop integrated into keeper and prevents door from swinging in beyond stile.

c.  	Bumper: Provided to prevent damage from door to panel or wall.

HIGH PRESSURE LAMINATE SUBSTRATE  (AccentSeries)

High Pressure Laminate Partitions with Stainless Steel Edge Trim:  Bobrick AccentSeries.

Color:  As selected by Architect from manufacturer’s standard AccentSeries range.

Color:  As indicated on Drawings.

Color:  As selected by Architect from manufacturer’s 10 Day RapidResponse AccentSeries range.

Color:  As selected by Architect from manufacturer’s 20 Day FastColor ClassicSeries range.

Color:  1500-60 Grey

Color:  1530-60 Beige

Color:  1572-60 Antique White

Color:  1595-60 Black

Color:  3690-58 Basalt Slate

Color:  4177-58 Lime

Color:  4622-60 Grey Nebula

Color:  4623-60 Graphite Nebula

Color:  4667-60 Green Tigris

Color:  4669-60 Natural Tigris

Color:  4674-60 Evening Tigris

Color:  4794-60 Windswept Bronze

Color:  4814-60 Tungsten Ev

Color:  4830K-18 Satin Stainless

Color:  4841-60 Desert Zephyr

Color:  4848-38 Pewter Mesh

Color:  4859-60 Spiced Zephyr

Color:  4924-38 White Carrara

Color:  5881-58 Chocolate Warp

Color:  5884-58 Chestnut Woodline

Color:  6212-58 Wheat Strand

Color:  6214-58 Seagrass Strand

Color:  6307-58 Burnt Strand

Color:  7018-58 Navy Grafix

Color:  7022-58 Natural Canvas

Color:  7040A-60 Figured Mahogany

Color:  7945K-38 Xanadu

Color:  851-58 Spectrum Blue

Color:  D30-60 Natural Almond

Color:  D307-60 Hollyberry

Color:  D315-60 Platinum

Color:  D321-60 Brittany Blue

Color:  D354-60 Designer White

Color:  D91-60 Slate Grey

Color:  D96-60 Shadow

Toilet Partitions:

Configuration:  Floor-Anchored partitions.

Basis-of-Design:  Bobrick 1531 AccentSeries Toilet Partitions.

Hardware:  Stainless steel hardware.

Configuration:  Floor-Anchored, Overhead-Braced partitions; extruded anodized aluminum with satin finish headrails, 0.045 inch (1.14 mm) thick with anti-grip profile.

Basis-of-Design:  Bobrick 1532 AccentSeries Toilet Partitions.

Hardware:  Stainless steel hardware.

Configuration:  Ceiling-Hung partitions, 10 ft (3048 mm) maximum ceiling height.

Basis-of-Design:  Bobrick 1538 AccentSeries Toilet Partitions.

Hardware:  Stainless steel hardware.

Fire Resistance:

Flame Spread Index (ASTM E 84):  60 for panels, doors and stiles.

Smoke Developed Index (ASTM E 84):  265 for panels, doors and stiles.

National Fire Protection Association/International Building Code Interior Wall and Ceiling Finish:  Class B.

Uniform Building Code:  Class II.

Urinal Privacy Screens:

Basis-of-Design:  Bobrick 1531 AccentSeries Floor-Anchored Urinal Privacy Screens.

Basis-of-Design:  Bobrick 1535 AccentSeries Wall-Hung Urinal Privacy Screens.

Basis-of-Design:  Bobrick 1538 AccentSeries Ceiling-Hung Urinal Privacy Screens.

Hardware:  To match partition hardware.

Fire Resistance:

Flame Spread Index (ASTM E 84):  60 for panels and stiles.

Smoke Developed Index (ASTM E 84):  265 for panels and stiles.

National Fire Protection Association/International Building Code Interior Wall and Ceiling Finish:  Class B.

Uniform Building Code:  Class II.

Dressing Compartments:  Floor-Anchored, Overhead-Braced.

Basis-of-Design:  Bobrick 1532 AccentSeries Dressing Compartments.

# a. 	Hardware: Stainless steel hardware.

Headrails:  Extruded anodized aluminum with satin finish, 0.045 inch (1.14 mm) thick with anti-grip profile.

Headrails:  Headrail with integral curtain tracks and hooks for compartments without doors.

Curtains:  Optional Bobrick vinyl curtains.

Fire Resistance:

Flame Spread Index (ASTM E 84):  60 for panels and stiles.

Smoke Developed Index (ASTM E 84):  265 for panels and stiles.

National Fire Protection Association/International Building Code Interior Wall and Ceiling Finish:  Class B.

Uniform Building Code:  Class II.

Finished Thickness:  1 inch (25 mm) for stiles, doors, screens and panels.  Finished thickness of doors and stiles to ensure flush front.

Materials:  3-ply, stiles, panels, doors, and screens.

Edge Trim:  18-8, type-304 stainless steel channel with satin finish.

Cores: 45 lb (20.4 kg) density, industrial grade, resin-impregnated, particle board.

Surfaces:  High Pressure Laminate ANSI/NEMA LD3-2005 minimum thickness 0.035 inch (0.89 mm).

Fabrication:  High Pressure Laminate bonded to core material with adhesive specially formulated to prevent delamination.  Edges bonded prior to bonding face sheets.  Splices or joints in faces or edges are not acceptable except in the case of laminate material limitations.

Stainless Steel Channels:  Mortised for flush fit with routed substrate.  Capped stainless steel channels fitted over surface of high pressure laminate not accepted.

Corners:  Mitered.

Wall Posts:  Pre-drilled for door hardware, 18-8, Type 304, 16 gauge (1.6 mm) stainless steel with satin finish; 1 inch (25 mm) x 1-1/2 inches (38 mm) x 58 inches high (1473 mm).

Stiles:  Floor-Anchored stiles furnished with expansion shields and threaded rods.

Overhead Braced Leveling Devices:  12 gauge, 3 inch x 1.25 inch (75 mm x 32 mm) zinc plated steel with chromate treatment; factory installed to bottom of stile.

Floor-Anchored / Ceiling-Hung Leveling Devices:  12 gauge, 1/2 inch x 1 inch (13 mm x 25 mm) steel channel welded to 3/8 inch x 1 inch (10 mm x 25 mm) zinc-chromate plated steel bar.

Stile Shoes:  One-piece, 22 gauge (0.8 mm), 18-8, Type 304 stainless steel, 4 inch (102 mm) height; tops with 90 degree return to stile.  One-piece shoe capable of adapting to 3/4 inch (19 mm) or 1 inch (25 mm) stile thickness and capable of being fastened (by clip) to stiles starting at wall line.

Anchors:  Expansion shields and threaded rods at floor connections as applicable.  Threaded rods secured to supports above ceiling as applicable.  Supports above ceiling furnished and installed as Work of Section 055000.

Hardware:  Concealed hardware.

Compliance:  Operable with one hand, without tight grasping, pinching, or twisting of the wrist, and force to operate does not exceed five pounds.

Emergency Access:  Hinges, latch allow door to be lifted over keeper from outside compartment.

Fastening:  Hinges secured to door and stile by stainless steel screws fastened into factory-installed, threaded inserts.  Fasteners secured directly into core not acceptable.

Mounting: Hinges, keepers, latches, clothes hooks and their fasteners concealed inside compartment.  Exposed hinges, keepers, latches, clothes hooks and their fasteners on exterior of compartment not acceptable with the exception of accessible compartments.

Mounting Brackets:  Mounted inside compartment; exposed brackets on exterior of compartment not acceptable with the exception of outswing doors.

Materials:  Stainless steel with satin finish for latches, hinges, coat hooks and bumpers, mounting brackets.  Chrome-plated “Zamak”, aluminum, or extruded plastic hardware not acceptable.

Latching:  Door is locked from inside by sliding door latch into keeper. Twist-style door latch operation not acceptable;

Doorstop:  Integrated into inswing latch to prevent doors from swinging out beyond stile; On outswing and alcove doors, doorstop integrated into keeper and prevents door from swinging in beyond stile.

Hinges:  Balanced, with field-adjustable cam to permit door to be fully closed or partially open when compartment is unoccupied.

Bumper:  Provided to prevent damage from door to panel or wall.

HIGH PRESSURE LAMINATE SUBSTRATE WITH STEEL CORE REINFORCED STILES (DesignerSeries)

High Pressure Laminate Partitions with Steel Core Stiles:  Bobrick DesignerSeries.

Color:  As selected by Architect from manufacturer’s standard DesignerSeries range.

Color:  As indicated on Drawings.

Color:  As selected by Architect from manufacturer’s 10 Day RapidResponse DesignerSeries range.

Color:  As selected by Architect from manufacturer’s 20 Day FastColor DesignerSeries range.

Color:  1500-60 Grey

Color:  1530-60 Beige

Color:  1572-60 Antique White

Color:  1595-60 Black

Color:  3690-58 Basalt Slate

Color:  4177-58 Lime

Color:  4622-60 Grey Nebula

Color:  4623-60 Graphite Nebula

Color:  4667-60 Green Tigris

Color:  4669-60 Natural Tigris

Color:  4674-60 Evening Tigris

Color:  4794-60 Windswept Bronze

Color:  4814-60 Tungsten Ev

Color:  4830K-18 Satin Stainless

Color:  4841-60 Desert Zephyr

Color:  4848-38 Pewter Mesh

Color:  4859-60 Spiced Zephyr

Color:  4924-38 White Carrara

Color:  5881-58 Chocolate Warp

Color:  5884-58 Chestnut Woodline

Color:  6212-58 Wheat Strand

Color:  6214-58 Seagrass Strand

Color:  6307-58 Burnt Strand

Color:  7018-58 Navy Grafix

Color:  7022-58 Natural Canvas

Color:  7040A-60 Figured Mahogany

Color:  7945K-38 Xanadu

Color:  851-58 Spectrum Blue

Color:  D30-60 Natural Almond

Color:  D307-60 Hollyberry

Color:  D315-60 Platinum

Color:  D321-60 Brittany Blue

Color:  D354-60 Designer White

Color:  D91-60 Slate Grey

Color:  D96-60 Shadow

Toilet Partitions:

Configuration:  Floor-Anchored partitions.

Basis-of-Design:  Bobrick 1041 DesignerSeries Toilet Partitions.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 1041.65 DesignerSeries Toilet Partitions.

Hardware:  Full-height stainless steel hardware.

Configuration:  Floor-Anchored, Overhead-Braced partitions; satin finish, extruded anodized aluminum headrails, 0.065 inch (1.65 mm) thick with anti-grip profile.

Basis-of-Design:  Bobrick 1042 DesignerSeries Toilet Partitions.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 1042.65 DesignerSeries Toilet Partitions.

Hardware:  Full-height stainless steel hardware.

Configuration:  Ceiling-Hung partitions, 10 ft (3048 mm) maximum ceiling height.

Basis-of-Design:  Bobrick 1048 DesignerSeries Toilet Partitions.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 1048.65 DesignerSeries Toilet Partitions.

Hardware:  Full-height stainless steel hardware.

Fire Resistance:

Flame Spread Index (ASTM E 84):  60 for panels, doors and stiles.

Smoke Developed Index (ASTM E 84):  195 for panels, doors and stiles.

National Fire Protection Association/International Building Code Interior Wall and Ceiling Finish:  Class B.

Uniform Building Code:  Class II.

Urinal Privacy Screens:

Basis-of-Design:  Bobrick 1041 DesignerSeries Floor-Anchored  Privacy Screens.

Basis-of-Design:  Bobrick 1043 DesignerSeries Post-to-Ceiling Urinal Privacy Screens.

Posts:  1.25 inch (32 mm) square, 18 gauge, (1.2 mm), Type-304 stainless steel, with satin finish.

Basis-of-Design:  Bobrick 1045 DesignerSeries Wall-Hung Urinal Privacy Screens.

Basis-of-Design:  Bobrick 1048 DesignerSeries Ceiling-Hung Urinal Privacy Screens.

Hardware:  To match partition hardware.

Fire Resistance:

Flame Spread Index (ASTM E 84):  60 for panels and stiles.

Smoke Developed Index (ASTM E 84):  195 for panels and stiles.

National Fire Protection Association/International Building Code Interior Wall and Ceiling Finish:  Class B.

Uniform Building Code:  Class II.

Dressing Compartments:  Floor-Anchored, Overhead-Braced.

Basis-of-Design:  Bobrick 1042 DesignerSeries Dressing Compartments.

Hardware:  Standard hardware.

Headrails:  Extruded anodized aluminum with satin finish, 0.065 inch (1.65 mm) thick with anti-grip profile.

Headrails:  Headrail with integral curtain tracks and hooks for compartments without doors.

Curtains:  Optional Bobrick vinyl curtains.

Fire Resistance:

Flame Spread Index (ASTM E 84):  60 for panels and stiles.

Smoke Developed Index (ASTM E 84):  195 for panels and stiles.

National Fire Protection Association/International Building Code Interior Wall and Ceiling Finish:  Class B.

Uniform Building Code:  Class II.

Finished Thickness:  1 inch (25 mm) for stiles, doors, screens and panels.  Finished thickness of doors and stiles to ensure flush front.

Materials:  3-ply, stiles, panels, doors, and screens.

Cores: 45 lb (20.4 kg) density, industrial grade, resin-impregnated, particle board.

Surfaces:  High Pressure Laminate ANSI/NEMA LD3-2005 minimum thickness 0.035 inch (0.89 mm).

Reinforcement:  Steel core stiles, 11-gauge (3.2mm) sheet steel reinforcement; leveling device welded to sheet-steel core of stiles.

Fabrication:  High Pressure Laminate bonded to core material with adhesive specially formulated to prevent delamination.  Edges bonded prior to bonding face sheets.  Splices or joints in faces or edges are not acceptable except in the case of laminate material limitations.

Wall Posts:  Pre-drilled for door hardware, 18-8, Type 304, 16 gauge (1.6 mm) stainless steel with satin finish; 1 inch (25 mm) x 1-1/2 inches (38 mm) x 58 inches high (1473 mm).

Stiles:  Floor-Anchored stiles furnished with expansion shields and threaded rods.

Leveling Devices:  3/8 inch x 7/8 inch (10 mm x 22 mm) steel bar welded to 11 gauge (3 mm) steel-reinforcing core; chromate-treated and double zinc-plated; welded to sheet-steel core of stiles.

Stile Shoes:  One-piece, 22 gauge (0.8 mm), 18-8, Type 304 stainless steel, 4 inch (102 mm) height; tops with 90 degree return to stile.  One-piece shoe capable of adapting to 3/4 inch (19 mm) or 1 inch (25 mm) stile thickness and capable of being fastened (by clip) to stiles starting at wall line.

Anchors:  Expansion shields and threaded rods at floor connections as applicable.  Threaded rods secured to supports above ceiling as applicable.  Supports above ceiling furnished and installed as Work of Section 055000.

Hardware:

Compliance:  Operable with one hand, without tight grasping, pinching, or twisting of the wrist, and force to operate does not exceed five pounds.

Emergency Access:  Hinges, latch allow door to be lifted over keeper from outside compartment.

Materials:  18-8, Type-304 stainless steel with satin finish for latches, hinges, coat hooks and bumpers, U-channels and mounting brackets. Chrome-plated “Zamak”, aluminum, or extruded plastic hardware not acceptable.

Fastening:  Hardware secured to door and stile by stainless steel machine screws fastened into factory-installed, threaded inserts.  Fasteners secured directly into core not acceptable.

Mounting: Hinges, keepers, latches, clothes hooks and their fasteners concealed inside compartment.  Exposed hinges, keepers, latches, clothes hooks and their fasteners on exterior of compartment not acceptable with the exception of accessible compartments.

Hardware Type:  Standard, commercial hardware.

Latching:  Track of door latch prevents inswing doors from swinging out beyond stile; on outswing doors, door keeper prevents door from swinging in beyond stile; 14 gauge (2 mm) sliding door latch, 11 gauge (3.2 mm) keeper.  Twist-style door latch operation not acceptable.

Hinges:  Balanced, with field-adjustable cam to permit door to be fully closed or partially open when compartment is unoccupied.

Locking:  Door locked from inside by sliding door latch into keeper.

Mounting Brackets:  Mounted inside compartment; exposed brackets on exterior of compartment not acceptable with the exception of outswing doors.

Hardware Type:  Continuous hardware (.65).

Latching:  Track of door latch prevents inswing doors from swinging out beyond stile; on outswing doors, door keeper prevents door from swinging in beyond stile; 14 gauge (2 mm) sliding door latch, 11 gauge (3.2 mm) keeper; latch slides on a shock-resistant nylon track. Twist-style door latch operation not acceptable.

Hinges:  16 gauge (1.6 mm) stainless steel with satin finish, self-closing, 3 section hinges.

Mounting Brackets:  18 gauge (1.2 mm) stainless steel and extend full height of panel.

U-Channels:  Secure panels to stiles.

Angle Brackets:  Secure stiles-to-walls and panels-to-walls.

HIGH PRESURE LAMINATE SUBSTRATE WITH STEEL CORE REINFORCED STILES AND STAINLESS STEEL EDGE TRIM (TrimLineSeries)

High Pressure Laminate Partitions with Steel Core Stiles and Stainless Steel Edge Trim:  Bobrick TrimLineSeries.

Color:  As selected by Architect from manufacturer’s standard TrimLineSeries range.

Color:  As indicated on Drawings.

Color:  As selected by Architect from manufacturer’s 10 Day RapidResponse TrimLineSeries range.

Color:  As selected by Architect from manufacturer’s 20 Day FastColor TrimLineSeries range

Color:  1500-60 Grey

Color:  1530-60 Beige

Color:  1572-60 Antique White

Color:  1595-60 Black

Color:  3690-58 Basalt Slate

Color:  4177-58 Lime

Color:  4622-60 Grey Nebula

Color:  4623-60 Graphite Nebula

Color:  4667-60 Green Tigris

Color:  4669-60 Natural Tigris

Color:  4674-60 Evening Tigris

Color:  4794-60 Windswept Bronze

Color:  4814-60 Tungsten Ev

Color:  4830K-18 Satin Stainless

Color:  4841-60 Desert Zephyr

Color:  4848-38 Pewter Mesh

Color:  4859-60 Spiced Zephyr

Color:  4924-38 White Carrara

Color:  5881-58 Chocolate Warp

Color:  5884-58 Chestnut Woodline

Color:  6212-58 Wheat Strand

Color:  6214-58 Seagrass Strand

Color:  6307-58 Burnt Strand

Color:  7018-58 Navy Grafix

Color:  7022-58 Natural Canvas

Color:  7040A-60 Figured Mahogany

Color:  7945K-38 Xanadu

Color:  851-58 Spectrum Blue

Color:  D30-60 Natural Almond

Color:  D307-60 Hollyberry

Color:  D315-60 Platinum

Color:  D321-60 Brittany Blue

Color:  D354-60 Designer White

Color:  D91-60 Slate Grey

Color:  D96-60 Shadow

Toilet Partitions:

Configuration:  Floor-Anchored partitions.

Basis-of-Design:  Bobrick 1031 TrimLineSeries Toilet Partitions.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 1031.65 TrimLineSeries Toilet Partitions.

Hardware:  Full-height stainless steel hardware.

Configuration:  Floor-Anchored, Overhead-Braced partitions; satin finish, extruded anodized aluminum headrails, 0.065 inch (1.65 mm) thick with anti-grip profile.

Basis-of-Design:  Bobrick 1032 TrimLineSeries Toilet Partitions.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 1032.65 TrimLineSeries Toilet Partitions.

Hardware:  Full-height stainless steel hardware.

Configuration:  Ceiling-Hung partitions, 10 ft (3048 mm) maximum ceiling height.

Basis-of-Design:  Bobrick 1038 TrimLineSeries Toilet Partitions.

Hardware:  Standard hardware.

Basis-of-Design:  Bobrick 1038.65 TrimLineSeries Toilet Partitions.

Hardware:  Full-height stainless steel hardware.

Fire Resistance:

Flame Spread Index (ASTM E 84):  60 for panels, doors and stiles.

Smoke Developed Index (ASTM E 84):  265 for panels, doors and stiles.

National Fire Protection Association/International Building Code Interior Wall and Ceiling Finish:  Class B.

Uniform Building Code:  Class II.

Urinal Privacy Screens:

Basis-of-Design:  Bobrick 1031 TrimLineSeries Floor-Anchored Urinal Privacy Screens.

Basis-of-Design:  Bobrick 1033 TrimLineSeries Post-to-Ceiling Urinal Privacy Screens.

Posts:  1.25 inch (32 mm) square, 18 gauge, (1.2 mm), Type-304 stainless steel, with satin finish.

Basis-of-Design:  Bobrick 1035 TrimLineSeries Wall-Hung Urinal Privacy Screens.

Basis-of-Design:  Bobrick 1038 TrimLineSeries Ceiling-Hung Urinal Privacy Screens.

Hardware:  To match partition hardware.

Fire Resistance:

Flame Spread Index (ASTM E 84):  60 for panels and stiles.

Smoke Developed Index (ASTM E 84):  265 for panels and stiles.

National Fire Protection Association/International Building Code Interior Wall and Ceiling Finish:  Class B.

Uniform Building Code:  Class II.

Dressing Compartments:  Floor-Anchored, Overhead-Braced.

Basis-of-Design:  Bobrick 1032 TrimLineSeries Dressing Compartments.

Hardware:  Standard hardware.

Headrails:  Extruded anodized aluminum with satin finish, 0.065 inch (1.65 mm) thick with anti-grip profile.

Headrails:  Headrail with integral curtain tracks and hooks for compartments without doors.

Curtains:  Optional Bobrick vinyl curtains.

Fire Resistance:

Flame Spread Index (ASTM E 84):  60 for panels and stiles.

Smoke Developed Index (ASTM E 84):  265 for panels and stiles.

National Fire Protection Association/International Building Code Interior Wall and Ceiling Finish:  Class B.

Uniform Building Code:  Class II.

Finish Thickness:  1 inch (25 mm) for stiles, doors, screens and panels.  Finished thickness of doors and stiles to ensure flush front.

Materials:  Edges are routed to allow flush fit of edge trim.

Edge Trim:  18-8, type-304 stainless steel channel with satin finish.

Reinforcement:  Steel core stiles, 11-gauge (3.2mm) sheet steel reinforcement; leveling device welded to sheet-steel core of stiles.

Cores:  45 lb density, industrial grade, resin-impregnated, particle board.

Surfaces:  High Pressure Laminate ANSI/NEMA LD3-2005 minimum thickness 0.035 inch (.89 mm) with matte finish.

Fabrication: High Pressure Laminate bonded to core material with adhesive specially formulated to prevent delamination.  Edges bonded prior to bonding face sheets.  Splices or joints in faces or edges are not acceptable except in the case of laminate material limitations.

Stainless Steel Channels:  Mortised for flush fit with routed substrate.  Capped stainless steel channels fitted over surface of high pressure laminate not accepted.

Corners:  Mitered.

Wall Posts:  Pre-drilled for door hardware, 18-8, Type 304, 16 gauge (1.6 mm) stainless steel with satin finish; 1 inch (25 mm) x 1-1/2 inches (38 mm) x 58 inches high (1473 mm).

Stiles:  Floor-Anchored stiles furnished with expansion shields and threaded rods.

Leveling Devices:  3/8 inch x 7/8 inch (10 mm x 22 mm) steel bar welded to 11 gauge (3 mm) steel-reinforcing core; chromate-treated and double zinc-plated; welded to sheet-steel core of stiles.

Stile Shoes:  One-piece, 22 gauge (0.8 mm), 18-8, Type 304 stainless steel, 4 inch (102 mm) height; tops with 90 degree return to stile.  One-piece shoe capable of adapting to 3/4 inch (19 mm) or 1 inch (25 mm) stile thickness and capable of being fastened (by clip) to stiles starting at wall line.

Anchors:  Expansion shields and threaded rods at floor connections as applicable.  Threaded rods secured to supports above ceiling as applicable.  Supports above ceiling furnished and installed as Work of Section 055000.

Hardware:

Compliance:  Operable with one hand, without tight grasping, pinching, or twisting of the wrist, and force to operate does not exceed five pounds.

Emergency Access:  Hinges, latch allow door to be lifted over keeper from outside compartment.

Materials:  18-8, Type-304 stainless steel with satin finish for latches, hinges, coat hooks and bumpers, U-channels and mounting brackets. Chrome-plated “Zamak”, aluminum, or extruded plastic hardware not acceptable.

Fastening:  Hardware secured to door and stile by stainless steel screws fastened into factory-installed, threaded inserts.  Fasteners secured directly into core not acceptable.

Mounting: Hinges, keepers, latches, clothes hooks and their fasteners concealed inside compartment.  Exposed hinges, keepers, latches, clothes hooks and their fasteners on exterior of compartment not acceptable with the exception of accessible compartments.

Hardware Type:  Standard, commercial hardware.

Latching:  Track of door latch prevents inswing doors from swinging out beyond stile; on outswing doors, door keeper prevents door from swinging in beyond stile; 14 gauge (2 mm) sliding door latch, 11 gauge (3.2 mm) keeper.  Twist-style door latch operation not acceptable.

Hinges:  Balanced, with field-adjustable cam to permit door to be fully closed or partially open when compartment is unoccupied.

Locking:  Door locked from inside by sliding door latch into keeper.

Mounting Brackets:  Mounted inside compartment; exposed brackets on exterior of compartment not acceptable with the exception of outswing doors.

Hardware Type:  Continuous hardware (.65).

Latching:  Track of door latch prevents inswing doors from swinging out beyond stile; on outswing doors, door keeper prevents door from swinging in beyond stile; 14 gauge (2 mm) sliding door latch, 11 gauge (3.2 mm) keeper; latch slides on a shock-resistant nylon track.  Twist-style door latch operation not acceptable.

Hinges:  16 gauge (1.6 mm) stainless steel with satin finish, self-closing, 3 section hinges.

Mounting Brackets:  18 gauge (1.2 mm) stainless steel and extend full height of panel.

U-Channels:  Secure panels to stiles.

Angle Brackets:  Secure stiles-to-walls and panels-to-walls.

EXECUTION

PREPARATION

Prepare substrates including but not limited to blocking and supports in walls and ceilings at points of attachment using methods recommended by the manufacturer for achieving the best result for the substrates under the project conditions.

Inspect areas scheduled to receive compartments for correct dimensions, plumbness of walls, and soundness of surfaces that would affect installation of mounting brackets.

Verify spacing of plumbing fixtures to assure compatibility with installation of compartments.

If preparation is the responsibility of another installer, notify Architect in writing of deviations from manufacturer’s recommended installation tolerances and conditions.

Do not proceed with installation until substrates have been properly prepared with blocking and supports in walls and ceilings at points of attachment and deviations from manufacturer’s recommended tolerances are corrected.  Commencement of installation constitutes acceptance of conditions.

INSTALLATION

Install products in strict compliance with manufacturer’s written instructions and recommendations, including the following:

Verify blocking and supports in walls and ceilings have been installed properly at points of attachment.

Verify location does not interfere with door swings or use of fixtures.

Use fasteners and anchors suitable for substrate and project conditions

Install units rigid, straight, plumb, and level.

Conceal evidence of drilling, cutting, and fitting to room finish.

Test for proper operation.

ADJUSTING, CLEANING AND PROTECTION

Adjust hardware for proper operation after installation.  Set hinge cam on in-swinging doors to hold doors open when unlatched.  Set hinge cam on out-swinging doors to hold unlatched doors in closed position.

Touch-up, repair or replace damaged products.

Clean exposed surfaces of compartments, hardware, and fittings.

END OF SECTION